## Slide 1: Summary overview report on Priority Gaps – Armour Assessment for year 2016
Neelam gupta, ccfe
WPMAT
MAT-1.3.1-T005-D002
It offers advantages in high melting point, high thermal conductivity, low thermal expansion and low-activation. On the other hand, it has high hardness and high brittleness, which is disadvantageous for the mechanical manufacturing of parts.

## Slide 2
Objective:
Develop structural design criteria for Plasma Facing Components and release the first issue of the DDC. This target is supported by two streams supporting tasks:
WBS1.3.1 – Priority Gaps
WBS1.3.2 – Enhancing Content and Usability
One of the priority gaps that has been identified is the definition of the assessment route required to ensure the appropriate structural integrity of the Armour element of a PFC.
Identify failure mechanisms for armor
Method:
SDC-IC Design rules studied and rules relevant to damage mechanism identified.
Literature review
Reviewed Abaqus extended finite element(XFEM) tool to carry out assessments
Deliverable:
Identify relevant Armour damage mechanisms.
Review the identified damage mechanisms and assess the validity of the available design rules and material properties. Highlight gaps and developmental areas.
Review and define an acceptable level of damage before the Armour is deemed to have failed.
Liase with professor Jeong-Ha Armour expert.
Write a end of year progress report, draft due 31ST October 2016, final due 31st December 2016.

## Slide 3
Armor -Overview
The primary purpose of the armor provided in the ITER first wall is to reduce plasma
contamination by sputtering erosion during normal operation and to reduce melting
and evaporation during plasma disruptions.
A secondary purpose of the protection layer, which is of interest to structural design,
is to prevent melting or other damage from occurring in the first wall structure.
No structural strength shall be attributed to the armor for satisfying the primary
Stress limits
Tungsten has been considered as the most promising armor material for PFCs in
fusion reactors such as first wall
Tungsten offers advantages in high melting point, high thermal conductivity, low
thermal expansion and low-activation. On the other hand, it has high hardness and
high brittleness, which is disadvantageous for the mechanical manufacturing of parts.

## Slide 4
Damage Mechanism of Tungsten Armor
Damage Mechanisms | Armor Element
Monotonic Damage | 
Plastic Collapse | 
Plastic Flow Localisation | x
Exhaustion of Ductility | Could be
Brittle Fracture | 
Thermal Creep | 
Cyclic Damage | 
Ratcheting | x
Fatigue | 
Environmental Damage | 
Swelling | x
Corrosion | 
Erosion | 
Compound Damage | 
Creep Fatigue | 

## Slide 5
Brittle fracture
Fracture will be a critical failure mechanism due to the limited ductility of the tungsten
below DBTT and due to the embrittlement by neutron irradiation.
Thus, the combination of brittleness and the thermally induced stress fields due to the
high heat flux loads raises a serious reliability issue in terms of the structural integrity of
tungsten armor.
SDC-IC Design rule
The design rules to prevent failure caused by insufficient fracture toughness at low
temperature, the elastic analysis limits(IC 3121.4.1) for k1/Kc as given below must be
satisfied.
If the elastic limit is not satisfied, elasto-plastic fracture mechanics methodology should
be used. The J-integral is an acceptable criterion for such cases and the following limits
be satisfied at all times.
Brittle fracture | Level A | Level C | Level D
Global (IC 3121.4.1.1) | 1=0.33 | 1=0.4 | 1=0.67
Local (IC 3121.4.1.2) | 2=0.67 | 2=0.8 | 2=0.90
 | Level A | Level C | Level D
Fracture (J1/Jc) | 1=0.67 | 1=0.8 | 1=0.9

## Slide 6
Brittle fracture (contd..)
In order to understand the mechanism of brittle cracking of tungsten armor and to predict tungsten’s
thermo-mechanical and fracture behaviours numerically,[1] could be a possible methodology for future guidance
for modelling the tungsten armor.
In this work ABAQUS - XFEM was employed for computing KI (or J-integral) and predicting progressive cracking,
respectively.
The model PFC considered for the FEM study is for a divertor with water-cooled tungsten monoblock duplex
structure consisting of a tungsten armor block and a CuCrZr alloy coolant tube (heat sink).
Thermo-mechanical elasto-plastic simulations wherein heat transfer problem was solved first, then its solution
was read into the corresponding mechanical simulation as a predefined temperature field.
Cross-rolled and stress-relieved tungsten was applied for the tungsten armor block.
For simulation, tungsten was assumed to be linear elastic and ideal-plastic. Temperature-dependent material
properties are utilised at selected temperatures, which correspond to the operation temperatures.
In the case of FW, a sandwich EUROFER blanket module coated with tungsten armor can be considered.
Data Required
The loading conditions relevant to DEMO first wall(both operational and shutdown conditions) is yet to be clearly
specified, but as a starting point the loading conditions of ITER divertor could be considered for assesment of
DEMO FW as this can be safely considered as conservative.
ITER material handbook provides the strength properties dependent on temperature for tungsten but the effect
of neutron irradiation has not been considered. Experimental campaign to better specify the effects of irradiation
on the strength and fracture property of tungsten is required.

## Slide 7
Fatigue
Tungsten armor under high heat flux load can suffer from deep cracking due to fatigue. This failure mechanism is under the umbrella of fatigue work carried by Mike Fursdon.
SDC-IC Design criteria
The applicable design rule for fatigue limit is provided in IC 3132.2.It states that when the component examined is not subjected to progressive deformation, the effects of the loading variations on fatigue damage accumulation can be estimated by the fatigue usage fraction.
The cumulative fatigue usage fraction at all points of the structure and for all cycles requiring compliance with levels A and C criteria overall operating periods must be less than1.
Assessment
There is some work done by [2] on tungsten failure due to low cycle fatigue. It is worth investigating as a "possible" methodology for future guidance in assessing tungsten armour.
In this work a two-stage modelling approach is employed where deep cracking is thought to be a consecutive process of crack initiation and crack growth, which is assumed to be caused by plastic fatigue and brittle facture, respectively.
The fatigue lifetime to crack initiation on the armor surface and the crack tip load of brittle fracture are assessed as a function of crack length and heat flux loads.
Commercial FEA code ABAQUS-XFEM was employed.
Data needed
ITER material handbook provides the LCF curves of two different tungsten grades (stress-relived and annealed). Experimental campaign to better specify the fatigue properties for irradiated tungsten.
Notes: To identify the threshold beyond which no proagation would occur.Experimental and numerical method.

## Slide 8
Erosion
The armor is subjected to in-service thinning resulting from surface erosion.
The thickness and erosion rate of the armor should be provided as an input.
If this is not available then in general, the analysis must check the temperature, thermal stress, damage due to fatigue and fracture for the FW structure considering different thickness of the tungsten armor.
Corrosion
If the FW is water cooled, there is a possibility of the FW structure being subjected to corrosion.
A crack propagation study should be carried out to assess the mechanism of the crack and the damage caused due to this.
Tests would be required to validate the behavior predicted numerically.
Erosion & Corrosion

## Slide 9
Thermal Creep
Tungsten, at relatively high (> ≈0.5 melting temperature) homologous temperatures,
could experience internal damage due to thermal creep, with or without environmental
interactions, by a variety of mechanisms, such as grain boundary cavitation, grain
boundary oxidation, etc.
Design criteria
To estimate the creep damage in a structure as a function of time, temperature, and
loading, a creep rupture usage function is computed and compared with the limits
imposed by IC 3221.2.3.
The procedure for determining creep rupture usage fraction based on time fraction
is calculated using the stress intensity ̅(IC 2766).This rule could be a good starting point
to adopt and the rule could be further improvised for the relevant component that is
analysed.
Data Required
Currently there is no material data to carry out the assessment of this damage
mechanism. The data that is required for the armor material are:
Creep rates
Creep rupture data
Creep-fatigue interaction data

## Slide 10
Thermal Creep
Tungsten, at relatively high (> ≈0.5 melting temperature) homologous temperatures,
could experience internal damage due to thermal creep, with or without environmental
interactions, by a variety of mechanisms, such as grain boundary cavitation, grain
boundary oxidation, etc.
SDC-IC Design criteria
To estimate the creep damage in a structure as a function of time, temperature, and
loading, a creep rupture usage function is computed and compared with the limits
imposed by IC 3221.2.3.
The procedure for determining creep rupture usage fraction based on time fraction
is calculated using the stress intensity ̅(IC 2766).This rule could be a good starting point
to adopt and the rule could be further improvised for the relevant component that is
analysed.
Data Required
Currently there is no material data to carry out the assessment of this damage
mechanism. The data that is required for the armor material are:
Creep rates
Creep rupture data
Creep-fatigue interaction data

## Slide 11
Creep fatigue
If the temperature is sufficiently high, creep deformation may occur during each cycle, accelerating the appearance of cracks by the process of creep-fatigue interaction.
This phenomenon is associated with thermal creep.
Irradiation-induced creep, discussed in IC2151, affects the stress-strain field but not the material damage. Time-dependent fatigue can also be the result of interactions between fatigue or creep fatigue with the environment, e.g., corrosion fatigue.
SDC-IC Design criteria
The applicable design rule for creep-fatigue interaction is specified in IC 3232.4 wherein Creep-fatigue damage is considered to be avoided if the summation of Fatigue usage fraction and Creep rupture usage fraction is less than Creep fatigue limit defined by creep fatigue interaction diagram.
In order to calculate the creep rupture usage fraction(IC 3221.2.3) stress intensity is multiplied by an arbitrary number.

## Slide 12
Results:
Damage mechanisms studied and identified relevant to armor.
Existing Design rules (SDC-IC) studied and relevant rules listed.
Highlighted some of the key data required to go ahead with the task
Approach for carrying out numerical studies which is a step towards design-by analysis
Conclusions:
Goals achieved
Identified relevant Armour damage mechanisms.
Reviewed the identified damage mechanisms and assessed the validity of the available design rules and material properties. Highlight gaps and developmental areas.
Write a end of year progress report, draft due 31ST October 2016
Goal not achieved
To Review and define an acceptable level of damage before the Armour is deemed to have failed. This would be continued next year.

## Slide 13
Midterm–Review: Objectives-Status for the 5 year period
Achievement and status:
Understanding extended finite element method (XFEM) as a potential methodology for fracture analysis given that crack propagation is an important damage mechanism for the armor. This method has been implemented to some of the standard problems to set guidelines for more complicated problems and future work.
Interaction of different damage mechanisms and its limits need to be further understood.
Would have been desirable if assessments were carried out using the methodology studied and been applied to design-by-analysis of an armor , even though the tungsten mono-block armor itself does not belong to the structural component
This methodology could be extended to a variety of applications such as the brazed joint.
Outlook:
To have a further understanding of the damage mechanism relevant to armor
Performing numerical study to assess important damage mechanism and applying it to design-by analysis within the framework of ITER SDC-IC
Challenge
The methodology is complex and cumbersome and yet has lot of potential. Implementation of this methodology for the assessments needs a dedicated resource.
lack of load specification, material database and sometimes lack of direction are the challenges

## Slide 14
References
Muyuan Li, Ewald Werner, Jeong-Ha You, Influence of heat flux loading
patterns on the surface cracking features of tungsten armor under ELM-like thermal
Shocks
2. Muyuan Li, Jeong-Ha You, Interpretation of the deep cracking phenomenon of
tungsten monoblock targets observed in high-heat-flux fatigue tests at 20 MW/m2,
Max-Planck-Institut für Plasmaphysik, Boltzmannstr. 2, 85748 Garching, Germany.

## Slide 15
Logos of the official WPMAT participants. Note: Some universities and labs are grouped in certain countries and, therefore, appear officially as only one RU (CIEMATand 2 sections of ENEA). Nevertheless, you are invited to add your own logo!