## Slide 1: Implementation of EDDI testing plan 2016 (KIT)
M. Walter, KIT
E. Gaganidze, KIT
WPMAT
TS-1.4.1-04
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching

## Slide 2
Objectives:
Evaluation and realization of required test series, identified and proposed by participating modellers.
Organization and Evaluation of round robin test campaigns (LCF-, tensile-, fracture-mechanical test series).
Methods:
Feasibility studies concerning proposed tests.
Performance of mechanical tests using suitable test facilities.
Deliverable:
Report on both the results of evaluations and the results of mechanical tests.
Acceptance Criteria:
If possible, tests will be performed according to standard specifications (ISO, ASTM etc).
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching IPP TS-1.4.1-04

## Slide 3
Results:
KIT organized the fabrication of different specimen charges (qty: 38/charge) used within the LCF round robin test campaign – the samples were manufactured at a local company (Hans Bischoff Feinmechanik GmbH, Keltern, Germany) according to the individual specifications of the different participating associations and after completion, sent to the respective labs (CIEMAT, ENEA-CNR, (KIT), NRG, SCK-CEN). The in-house LCF test campaign is under way.
Within the frame of the fracture-mechanical round robin test, KIT performed 3-point-bending tests on EUROFER97-2 at room temperature on common sized specimens with rectangular cross-section (89x18x15 mm3). It is found, that the used sample type is not suitable for determining valid fracture toughness values of EUROFER97 according to ASTM E1820 (Jlimit=b0sc/7.5 not fulfilled).
KIT agreed to perform fracture mechanical fatigue tests on CuCrZr samples in order to verify a new design rule for DEMO, developed at CCFE. The tests will be conducted in the first quarter of 2017.
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching IPP TS-1.4.1-04

## Slide 4
Outlook:
(Completion of the in-house LCF test campaign).
Realization of the fracture-mechanical fatigue tests on CuCrZr samples.
Evaluation of the different round robin test results.
Evaluation of possible new proposals …
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching IPP TS-1.4.1-04
Conclusions:
KIT provided different LCF specimen charges within the frame of the LCF round robin test campaign.
KIT performed 3-point-bending tests at RT within the frame of the fracture-mechanical round robin campaign.
KIT agreed to perform fracture-mechanical fatigue tests in 2017 on CT-specimens from CuCrZr in order to verify a new design rule for DEMO.

## Slide 5
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching IPP TS-1.4.1-04
Objective:
In order to determine material parameters of advanced design codes, the main objective of the work is to provide missing mechanical characteristics of DEMO/ITER relevant structural materials. For this purpose, on the one hand, required test series, identified and proposed by participating modellers, must be evaluated – and if possible, performed. On the other hand, based on the participation of several experimental groups from different European associations, a coordination of such tests series with respect to the general availability of test facilities within the different labs has to be realized.
To ensure that the experimental devices of the different participating labs deliver comparable results, until now the work is mainly focussed on organizing and evaluating round robin (RR) test campaigns dealing with tensile-, fracture-mechanical- and low cycle fatigue (LCF) experiments.
Midterm–Review: Objectives-Status for the 5 year period

## Slide 6
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching IPP TS-1.4.1-04
Activities:
Members of EDDI were asked to propose tests, neccessary for determining missing material parameters.
Based on boundary conditions, specified by ENEA-CNR and KIT, several European labs agreed to participate within the frame of different round robin campaigns (tensile-, fracture-mechanical- and low cycle fatigue experiments). In order to ensure that the obtained results are only affected by the individual approaches of the labs when performing a special kind of test, KIT generally provided the material (standard heat treated EUROFER97-2) in the case of the tensile- and fracture-mechanical round robin test campaigns (summer 2015), and based on the effect of surface conditions on the lifetime, complete specimen charges (again fabricated from standard heat treated EUROFER97-2) in the case of the low cycle fatigue round robin test campaign (spring 2016). All participants were asked to complete both the tensile tests and the fracture-mechanical tests up to the end of 2015 as well as to complete the LCF tests up to the end of 2016 and to provide the obtained results promptly.
Midterm–Review: Objectives-Status for the 5 year period

## Slide 7
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching IPP TS-1.4.1-04
Current status:
KIT (J. Aktaa) proposed to perform combined low cycle fatigue tests and creep tests on EUROFER97 samples (specified LCF tests up to a certain number of cycles followed by specified creep tests) in order to determine creep properties of already softened material. Furthermore, CCFE (M. Fursdon) proposed to perform fracture mechanical fatigue tests on CT samples from CuCrZr in order to verify a new design rule for DEMO. After evaluation it was decided that ENEA-CNR will perform the tests proposed by J. Aktaa (already started) and KIT will perform the tests proposed by M. Fursdon (will start at the beginning of 2017).
KIT performed both tensile tests and fracture-mechanical tests within the respective round robin test campaigns and provided the results. The fatigue tests within the frame of the LCF round robin campaign are under way.
Up to now, none of the round robin test campaigns could be evaluated. Even results from tensile tests are missing.
Midterm–Review: Objectives-Status for the 5 year period

## Slide 8
WPMAT EDDI Monitoring Meeting 3.-4.11.2016 Garching IPP TS-1.4.1-04
Outlook:
If necessary, completion of the in-house LCF test campaign.
Realization of the fracture-mechanical fatigue tests on CuCrZr samples.
Evaluation of the different round robin test results.
Evaluation of possible new proposals.
Midterm–Review: Objectives-Status for the 5 year period

## Slide 9
EDDI Round Robin Test Campaigns Participants